Supporting Information

- Fig. S1. XRD patterns of ZrW2O8 after calcination at different temperatures and for different durations under Ar atmosphere

- Fig. S1 presents the XRD patterns of pure ZrW2O8 calcined at different temperatures and holding times in an Ar atmosphere. The results show that ZrW2O8 remains stable below 700 ℃ without obvious decomposition products. When the temperature reaches 700 ℃, characteristic diffraction peaks of ZrO2 and WO3 appear, indicating the decomposition of ZrW2O8.

- Fig. S2. XRD patterns of MSABs adhesive doped with different concentrations of ZrW2O8 after calcination at various temperatures in Ar atmosphere (a: 40 wt.%; b: 60 wt.%)

- Fig. S2 presents the XRD patterns of 40 wt.% and 60 wt.% ZrW2O8-modified MSABs adhesives after heat treatment at 700-900 ℃. The adhesives with different modification contents exhibit consistent phase evolution behavior: the main phase is incompletely decomposed ZrW2O8 at 700 ℃; ZrW2O8 decomposes significantly to form ZrO2, WO2, and WO3 at 800 ℃; and new phases such as AlPO4 and SnxWO3 are formed at 900 ℃. As the ZrW2O8 modification content increases from 40 wt.% to 60 wt.%, the intensities of the characteristic diffraction peaks of the decomposition products ZrO2, WO2, and WO3 gradually increase, indicating that a higher ZrW2O8 dosage promotes the formation of decomposition products.

- Fig. S3. FT-IR patterns of MSABs adhesive doped with different concentrations of ZrW2O8 after treatment at various temperatures (a: 40 wt%; b: 60 wt%)

- Fig. S3 displays the FT-IR spectra of MSABs adhesives modified with 40 wt.% and 60 wt.% ZrW2O8 after calcination at 700-900 ℃. The W-O-Zr peak at 885 cm-1 gradually weakens and the W=O peak emerges with rising temperature, indicating the progressive decomposition of ZrW2O8. Notably, the B-O peak at 1367 cm-1 exhibits concentration-dependent evolution: it is insignificant at 700 ℃ and only prominent at 800-900 ℃ for the 40 wt.% ZrW2O8-modified MSABs, while it is clearly observable at all three temperatures for the 60 wt.% ZrW2O8-modified MSABs. This is because  higher ZrW2O8 content introduces more lattice defects and heterogeneous interfaces to accelerate B4C oxidation kinetics. The Si-O peak at 448 cm-1 reflects the ceramization process of the silicone resin matrix.

- Fig. S4. TG-DSC curves of different adhesives from room temperature to 800 ℃ (a: 40 wt.%; b: 60 wt.%)

- Fig. S4 presents the TG-DSC curves of 40 wt.% and 60 wt.% ZrW2O8-modified MSABs adhesives from room temperature to 800 ℃. Within 400-800 ℃, the 40 wt.% ZrW2O8-modified MSABs shows a continuous mass loss up to 8.25%, while the 60 wt.% ZrW2O8-modified MSABs stabilizes at 6.60% after 700 ℃. The 40 wt.% ZrW2O8-modified MSABs exhibits multiple exothermic peaks, whereas the 60 wt.% ZrW2O8-modified MSABs shows a single exothermic peak. Higher ZrW2O8 content effectively compensates for mass loss and restrains resin exothermic oxidation, an effect absent in the 40 wt.% ZrW2O8-modified MSABs due to insufficient modification.